Table 1: Summary statistic for and resin canal features in xylem of 2-year-old P. radiata clones and families.

|  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Variable | Plant type | Mean | 95%  Confidence Interval | | P-value of the difference between means | Coefficient of variation |
| Lower | Upper |
| Resin canal density (number/mm2) | Clone | 0.69 | 0.65 | 0.73 | 4.73e-12 | 31.4 |
| Family | 0.90 | 0.87 | 0.94 | 27.8 |
| % Resin canal area | Clone | 1.13 | 1.06 | 1.20 | 1.95e-14 | 30.7 |
| Family | 1.53 | 1.47 | 1.59 | 28.3 |
| Resin canal size (mm2) | Clone | 0.0165 | 0.0161 | 0.0169 | 0.0186 | 11.9 |
| Family | 0.0170 | 0.0168 | 0.0173 | 10.1 |